## Slide 1: Experimental methods in mechanics of solids
Role of experiments in stress-strain analyses and in assessment of failure risk:
  to acquire input data for computations (material characteristics, limit values of the relevant quantities, assessment of the character and magnitude of loads),
  to verify the results of computational models,
  to obtain some results in the fields of problems, where no computational modelling is possible (problems of abrasion, corrosion, erosion, cavitation, pitting etc.).
Conclusion: no computation can exist without experiments.

## Slide 2: Systemization of measuring methods in the mechanics of solids
methods for evaluation of stresses and strains,
methods for monitoring of the fracture process,
methods for evaluation of the body movements,
incl. its deformational displacements,
methods for evaluation of external loads acting upon bodies.
Warning! It is impossible to measure stresses directly!!!
The evaluation of stresses is always based on calculations:
Strains can be measured directly or calculated from the measured displacements. For the calculation of stresses, knowledge of constitutive relations and their parameters is necessary.
To obtain the constitutive relations (between stresses and strains) and their parameters, some basic mechanical tests are necessary. In these tests the stress values are calculated on the basis of the measured force and some assumptions on the stress distribution (uniaxial tension, bending, etc.).

## Slide 3: Overview of basic methods for stress and strain experimental evaluation
Tensometry – the most frequent method in practical applications. In contrast to other methods it is local, it does not measure a strain field (strains in the whole body or on its whole surface) but only the change of a specified length, which is recalculated into the average strain value specific for the gauge location. Therefore the accuracy depends on the gauge size and on the strain gradient.
Photoelasticimetry – a complex experiment with a transparent model using a polarized light. It is based on the photoelastic effect: some transparent material become optically anisotropic under load.
Brittle laquers – based on the low ultimate strain of some resins, which crack at a certain value of strain. These strain indicating lacquers (or films) are advantageous for finding dangerous locations of the body and the directions of the maximum principal strain (stress) here.
Moiré method – is based on the light interference when passing diffraction lattices; the difference between the deformed and reference lattices creates the moiré strips corresponding to displacements equal to the lattice span.
Holografic methods - based on the laser light interference between the hologram of an undeformed body and the real deformed body. The created interference strips are proportional to the displacement magnitude. Disadvantage – an accurate mutual positioning of the hologram and the body is extremely difficult.
Radiographic strain measuring – is based on the diffraction of a monochromatic X-radiation on the crystallic lattice (with span on the order 10-10 m), which acts as a diffraction lattice.
Stress Pattern Analysis (SPATE method) – it exploits the transformation of the strain energy into heat. It evaluates temperatures in different points of the body under conditions of repeated deformation caused by a cyclic loading.

## Slide 4: Photoelasticimetric image of a gear tooth
Isochromats
– lines connecting points with an identical difference between principal stresses

## Slide 5: Examples of application of brittle laquers with U-shaped profiles under various loads

## Slide 6: Examples of application of brittle laquers
Piston rod and bearing pin under torsion
Vanes of a compressor impeller wheel

## Slide 7: Principle of moiré method
orientation of the lattice
reference lattice
measuring lattice
investigated body
ilumination
measuring lattice
screen

## Slide 8: Examples of simple moiré strips (contour lines)
Uniform uniaxial tension
Local maximum of displacements
Loading by an isolated force
Local minimum of displacements

## Slide 9: Holografic interferometry
In real time application, this method is based on interference of a laser beam between the hologram of the undeformed body and the real deformed body. The created interference strips are proportional to the displacement magnitudes.
The interference strips in the figure are created by vibrations of a circular plate.

## Slide 10: Radiographic strain measuring
The diffraction of the X-radiation can be interpreted as a reflection of beams by crystallographic planes, which acts as a diffraction lattice. Spots with maximal and minimal intensity of the reflected radiation depend on their distance; when these distances (with their span on the order of 10-10 m) are changed by the load, a change in diffraction images occurs.
primary
beam
reflected
beam
body surface
atomic
plane

## Slide 11: Types of strain gauges (tensometers)
Mechanical strain gauges – they use sharp contact edges or tips, basement length typically tens of mm.
String strain gauges – a change in the string tension changes the frequency of string vibrations, basement lengths of 50-400 mm, applications mostly in civil engineering (dams).
Pneumatic strain gauges – the mutual positions of jet and flap (in a distance of mm) are controlled by sharp edges, the distance influences the air pressure in front of the jet.
Electric strain gauges
  resistance strain gauges – the change of the electric resistance of the sensor as a consequence of changes in its length, the most frequent in technical practice,
  semiconductor strain gauges – based on the piezoresistive effect, more sensitive ,
  inductivity strain gauges – basement length tens of mm, the change in position is transformed into a change of inductivity,
  capacitor strain gauges - the change in position is transformed into a change of the capacity of a capacitor.

## Slide 12
Leads
Cover
Measuring grid
Grid length
carrier
Grid width
Electric resistance strain gauges

## Slide 13
Principle:
l
l
F
F
l/l0
F=0
l0
stress
elongation
Notes: <number>
Charakteristika

## Slide 14
HBM, Thomas Kleckers (August 1999)
Gauge factor k: sensitivity of the gauge
R/Ro = k 
R/Ro = k * 
A strain gauge converts a mechanical
strain into a change of the gauge electrical resistance
Notes: <number>
4

## Slide 15
Basic types of strain gauges
Uniaxial gauge
(for uniaxial stress)
T-rosette
(right gauge - for biaxial stresses with known principal directions)
Rosette
(for biaxial stresses with unknown principal directions)
Strain measuring chain
Notes: <number>
Charakteristika

## Slide 16: Methods for monitoring the fracture process
The most frequent methods for monitoring the fracture process are as follows:
Acoustic emission
Crack detection by conducting paints
Crack propagation monitoring by plastic films
Crack detection by penetrating paints
Sources of the acoustic emission can be as follows:
Initiation and development of microdefects.
Phase (crystallic) transformations in material.
Plastic deformation related to the initiation of slip bands or to an intensive dislocation movement.
Ruptures of reinforcing fibers in composite materials, as well as separation between fibres and matrix, delamination, etc.
An existing fracture can be analyzed by methods of fractography.

## Slide 17: Detection of the body movement
The measured quantities can be of the following types:
displacement (change in position)
velocity
acceleration.
With respect to the reference system, the displacement can be
  displacement of the body as a whole,
  displacement caused by a body deformation.
Deformation displacements use to be periodical (vibrations).

## Slide 18: Basic types of sensing elements for movement detection
Piezoelectric sensing elements detect the acceleration.
They are based on the piezoelectric properties of some crystals able to induce an electric charge proportional to the load of the crystal. The load – force acting upon the crystal – is proportional to the acceleration (according to Newton’s law F = m.a), so that the voltage on the crystal is proportional to the acceleration. These elements are suitable for detection of fast dynamic processes.
Inductivity sensing elements detect the position or velocity.
  Inductivity (the electric resistance of the coil under alternating voltage) can be changed in consequence of changes of the airspace width in a magnetic circuit or by sliding of the core into the coil (it detects changes of position).
  A coil movement in a magnetic field induces a voltage (proportional to the velocity component perpendicular to the magnetic flux lines) in the coil – the velocity of movement is detected..
Inductivity sensing elements have a higher centrifugal mass, therefore they are not suitable for detection of fast dynamic processes.
Capacitor sensing elements detect the change of position.
They are based on a change of the capacity caused by change in the distance of capacitor plates (electrodes) or by change in their overlapping. They are able to detect very fast changes and, as contactless sensors, they are suitable for detection of vibrations of rotating or fast moving bodies.
Tensometer sensing elements are based on detection of the deformation of a body, mostly a beam or membrane, using resistance metalic or semiconductor strain gauges. The measured strain can be recalculated into displacements of the substrate (beam or membrane).

## Slide 19: Tensometer position sensing element
Tensometer sensing element

## Slide 20: Sensing elements for measuring of loads
Loads to be measured can be represented by:
  forces,
  moments (couples),
  pressure.
Principles of sensing elements:
  tensometer – the required load magnitude is calculated using the linear theory of elasticity from the strain value measured in the defined location on the sensing element surface by an electric resistive strain gauge,
  piezoelectric,
  inductivity,
  capacitor.